## Slide 1: Electrochemical Techniques in Materials Science and Engineering
A.C. Bastos
acbastos@ua.pt

## Slide 2
Objective
Contents
Short illustration on how electrochemical techniques can be used to characterise novel materials and help identify new functions and applications.
- A glimpse of electrochemistry
- Applications in science and technology
- Examples of the use of electrochemical techniques in
the research and development of new materials:
- Cyclic Voltammetry
- Electrochemical Impedance Spectroscopy (EIS)
- Microelectrodes

## Slide 3
Electrochemistry
Electrochemistry studies the chemical phenomena involving electricity.
Historically it is considered to have begun in 1800 with the Alessandro Volta pile.
Applications evolved fast.
1800 Water electrolysis (Nicholson and Carlisle, England; Ritter in Poland).
1802/4 In England, Wollaston discovers Pa and Ro, Tennant discovers Ir and Os.
1805 Luigi Brugnatelli (Italy) invents electrodeposition (deposited gold).
1807/8 Humphry Davy (England) discovers Li, K, Na, Ca, Mg by electrolysis of molten salts with a battery with 2000 elements.
1838 Jacobi (Germany) invents galvanoplasty (electrotyping).

## Slide 4
- Refining of metals
- Electrosynthesis
- Surface treatments
- Corrosion protection
Industry
Analytical
Chemistry
Electrochemistry today
Life sciences
- Batteries
- Accumulators
- Fuel cells
- Solar cells
- Supercapacitors
Energy
Environment
- Soil decontamination
- CO2 valorisation
- Water treatment
- Elimination of pollutants

## Slide 5
Reduction-oxidation reactions (redox reactions) are chemical reactions where one species looses electrons (oxidizes) and another species gains electrons ( iis reduced). The half- -reactions (oxidation and reduction) can occur separated in space.
Electrochemistry
Overall reaction: Ox1 + Red2  Red1 + Ox2
Reduction (cathode): Ox1 + ne-  Red1
Oxidation (anode): Red2  Ox2+ ne-
Example: Cu2+ + Fe  Fe2+ + Cu
Red: Cu2+ + 2e-  Cu
Ox: Fe  Fe2+ + 2e-
Spontaneous (galvanic) process
With a power source
(electrolytic process)

## Slide 6
Charge transfer
Faradaic current
Electrical double layer
Capacitive current
Equivalent electric circuit

## Slide 7
Key quantities
Electrode potential, E (Vvs reference)
Electrical current, I (A)
Current density, i (A m-2)
Charge, Q (C)
Time, t (s)
Current density is more important:
Electrochemistry
Current is a RATE:
Charge is an AMOUNT:

## Slide 8
Electrode Potential scales
Electrochemistry
3 electrode cell

## Slide 9
New
material
Electrochem. properties
Conductive?
Reversible?
Potential window?
ORR
OER
ORR - oxygen reduction reaction
OER - oxygen evolution reaction
Supercaps - supercapacitors
Supercaps
Removal
of pollutants
Fuel cells
Sensors
Electro- -synthesis
Energy
Environment
C a t a l y s t
We have a new material.
Now what?

## Slide 10
Cyclic voltammetry
Reversible vs irreversible
Hexacyanoferrate(II)
Hexacyanoferrate(III)

## Slide 11
1. Conductivity (using a simple DMM)
Good? Acceptable?
3. Working potential window
Good? Acceptable?
Electrochim. Acta 76 (2012) 487
2. Check electrochemical response.

## Slide 12
Electrochim. Acta 76 (2012) 487
Boron doped diamond (BDD) microelectrodes
for detection of Zn2+ and O2 in water
Another application for this material:
oxidation of pollutants dissolved in water (electrodes with large area)
Detection of Zn2+
Detection of dissolved O2
Fe-Zn galvanic cell

## Slide 13
Reduced graphene oxide on paper substrate
Not good catalysts…
…but maybe still OK as materials for supercapacitors or potentiometric sensors.

## Slide 14
Supercapacitors
Vertically aligned carbon nanotubes (VACNTs) grown directly on pretreated Inconel® metallic substrate by thermal CVD
J Mater Chem A 3(2015)17804

## Slide 15
Calcined PU foams
- High resistance
(increasing calcination temperature decreases the resistance but then brittleness increases).
- Bad cyclic voltammograms
(irreversible response)
Potentiometric response to pH
Linear response to pH but slope is
33-37 mV/pH unit where it should be 59 mV/pH unit

## Slide 16
CoPt3 Nanoparticles
GC disk with a dried drop of the dispersion.
    2 µL suspension
    (4 ng of NP)
    +
    2 µL of Nafion 0.05 wt.% in ethanol
Working electrode (WE):
NPs on GC RDE.
Reference Electrode (RE):
Hg|Hg2SO4|K2SO4(sat)
(E = +0.651VRHE; E = +0.409VSCE)
Counter Electrode (CE):
Platinum wire
Electrolyte:
0.5M H2SO4
Bubbling of gas:
Argon or O2
CE
WE
(RDE)
RE
Gas bubbling
0.5M H2SO4
RDE motor
Gas inflow
RE
CE

## Slide 17: Cyclic voltammetry with O2 in solution (saturation)
5 mV/s in O2 saturated 0.5M H2SO4
at room temperature and 1600 rpm.
5 mV/s in O2 saturated 0.1 M HClO4
at toom temperature and 1600 rpm.
Nature Materials 12 (2012) 81.

## Slide 18: Cyclic voltammetry without O2 in solution (Ar bubbling)
50 mV/s in Ar saturated 0.1 M HClO4
at 60 °C and 1600 rpm.
50mV/s in Ar saturated 0.5M H2SO4
at room temperature and 1600 rpm.
~350 mV
~100 mV
ACS Catalysis 1 (2011) 1355.
Decrease in current: poisoning or surface deactivation.

## Slide 19
The simplest representation of the electrode-solution interface
Electron transfer
Electrical double layer
f
θ-
Nyquist plot
-Z”vs Z’
Bode plot
log |Z| vs log f
 vs log f
 = 2 f
Electrochemical Impedance Spectroscopy (EIS)

## Slide 20
Impedance of a painted metal
while it degrades
1. Intact film
Rs
Cf
paint
metal
Rs
Cf
Rpo
2. Conductive pathways through the film
Rpo
Rs
Rct
Cdl
Cf
3. corrosion
Rs – solution resistance
Rpo – paint (pore) resistance
Cf – paint film capacitance
Rct – charge transfer resistance
Cdl – double layer capacitance
Rpo
Rct
Cdl
Cf

## Slide 21
Impedance of aluminium alloy 2024-T3 immersed in 0.05M NaCl
μA cm-2
30 min
1 day
1 week
1 month
1 mm
EIS

## Slide 22
- Can probe small volumes of solution
- Provide spatial resolution
- Can be placed very close to the surface
Microelectrodes
SRET – Scanning Reference Electrode Technique
SVET – Scanning Vibrating Electrode Technique
LEIS – Localised Electrochemical Impedance Spectroscopy
SIET – Scanning Ion Selective Electrode Technique
SECM – Scanning Electrochemical Microscopy
WBE – Wire Beam Electrode
SKP – Scanning Kelvin Probe
SKPFM – Scanning Kelvin Probe Force Microscopy
AFM – Atomic Force Microscopy

## Slide 23
10 mm
vibrating
probe
Scanning Vibrating Electrode Technique
(SVET)

## Slide 24
Electrogalvanised steel 1 day in 0.05M NaCl
1 mm

## Slide 25
Electrogalvanised steel 1 day in 0.05M NaCl

## Slide 26
DC04 low carbon steel in 0.05 M NaCl

## Slide 28
Micro-potentiometry (SIET)
Ref. electrode
Ion- Selective Microelectrodes
1 cm
glass micropipette
Ag wire with AgCl coat
Filling solution:
0.005M NaCl
76 µm
sensitive ionophore gel

## Slide 29
pH map
Etched AA2024-T3 after 24 houras in 0.005 M NaCl
Pits
1 mm
1 cm
pH

## Slide 30
Degradation (corrosion) of bioglass in SBF solution
Ca2+
Na+
Mg2+
pH
Work ongoing
z
x
y
Flux (mol s-1 m-2)

## Slide 31
e-
OH-
H+
H2O + 2h+  1/2O2 + 2H+
1/2O2 + H2O + 2e-  2OH-
2H2O + 2e-  H2 + 2OH-
Oxidation
Redution
Water splitting in TiO2 nanotubes
investigated with microelectrode techniques

## Slide 32
1 mm
Water splitting in TiO2 nanotubes
investigated with microelectrode techniques
Irradiated spot
UV LED (365 nm)
< 5 mW cm-2
μA cm-2
μA cm-2
TiO2 nanotubes
0.1M Na2SO4
SVET map before irradiation
(no current)
SVET map during irradiation
(anodic spot, remaining area slightly cathodic)

## Slide 33
Top view
Bright side
Dark side
Epoxy mount
Side view
Masking
wax
0.05M Na2SO4
Adhesive
tape
UV
Short-circuit
Potentiostat
Water splitting in TiO2 nanotubes
investigated with microelectrode techniques
SVET
SIET

## Slide 34
Conclusions

## Slide 35
Presentation template by SlidesCarnival (www.slidescarnival.com)