## Slide 1: THE SEPARATION OF ANODIC AND CATHODIC DEFECTS ON ORGANIC COATINGS
A.C. Bastos, M.C. Quevedo, M.G.S. Ferreira
AETOC2015
La Rochelle, France
22-25 Abril 2015

## Slide 2
8.5mm
Epoxy clearcoat on carbon steel; 0.1M NaCl
Context
μA cm-2
0
3.2
0
3.3
1.6
1.65
X / mm
Y / mm
1mm
10 minutes
1mm
μA cm-2
0
1.5
0
1.4
0.75
0.7
X / mm
Y / mm
1 hour
0
1.5
0
1.4
0.75
0.7
X / mm
Y / mm
25 min

## Slide 3
1mm
phenolftalein
0
3.1
0
2.8
1.55
1.4
X / mm
Y / mm
μA cm-2
Scan starts with both defects exposed.
At the middle of the scan (point 200 in a map of 20x20 points) the anodic defect was covered. Cathodic activity immediately disappeared.
beginning
end
0
3.1
0
2.8
1.55
1.4
X / mm
Y / mm

## Slide 4
1mm
μA cm-2
μA cm-2
μA cm-2
0
3.1
0
2.8
1.55
1.4
Y / mm
0
3.1
0
2.8
1.55
1.4
X / mm
0
2
0
2
1
1
10 minutes after separation
50 min
3h40
1mm
1mm

## Slide 5
Painted HDG
(SVET, Zn2+)
Electrochem. Commun. 12 (2010) 394
More examples…

## Slide 6
Sol-gel coated AZ31 magnesium alloy
(SVET, pH, Mg2+)
Electrochem. Commun. 10 (2008) 259
More examples…

## Slide 7
5 µA cm-2
500 µm
19 hours in
0.05 M NaCl
More examples…
Sol-gel coated 2024 aluminium alloy
(SVET, pH, O2)
Electroanalysis 22 (2010) 2009

## Slide 8
Electroanalysis 22 (2010) 2009
More examples…
Sol-gel coated 2024 aluminium alloy
(SVET, pH, O2)
500 µm
lines

## Slide 9
The techniques
Scanning Vibrating Electrode Technique
vibrating
probe
Ground and pseudo
reference
electrode
10 mm
vibrating
probe
Micro-potentiometry (pH)
Micro-amperometry (O2)
10 µm Pt wire
platinum
microdisc
electrode
reference
electrode
pre-amplifier
head
region of diffusion
control
Voltammogram for the reduction of dissolved oxygen in 0.05M NaCl
1 cm
glass micropipette
Ag wire with AgCl coat
Filling solution:
0.1M KCl + 0.01M KH2PO4
25 µm
pH sensitive ionophore FLUKA ref. 95293
r2=0.997
Potentiometric response with commercial pH buffers.
ISME
RE
sample
1 cm

## Slide 10
“Pure” Fe
250 μm
Min
12h
6h
1h
Min
12h
6h
1h
500 μm

## Slide 11
Fe twin electrodes
Current flowing between Fe-Fe (ZRA)
O2 + 2H2O + 4e- → 4OH-
For a 1mm Fe-Fe
n =4 (2-4)
F = 96485 C mol-1
DO2 = 2.01 x 10-5 cm2 s-1
CO2 = (2.4 x 10-7 mol cm-3
A = 7.85 x10-3 cm2
δ = 325 µm (132 µm if n=2)
Cathodic control
O2 reduction at the non corroded Fe
“passive” Fe
“corroded” Fe
pH and dissolved O2
above both Fe
pH
O2
measurements 50 μm above surface
250 μm

## Slide 12
Fe twin electrodes
What can be expected?
Polarization curves of the twin Fe electrodes immediately after breaking the connection
Polarization curves of Fe electrodes in 0.05M NaCl
At pH=6 and pH=10.

## Slide 13
Fe twin electrodes
The polarization curves were repeated with the twin electrodes connected and the current measured with the SVET probe directly above either the “passive” or the “corroded” Fe electrodes.
1 mm

## Slide 14
OCP (-0.72 V)
-0.62 V
-0.3 V
-0.5 V
-0.72 V
-0.62 V
-0.5 V
-0.3 V

## Slide 15
What do we know so far?
Does it always occur?
For how long does the separation remain?
It is possible to explain how the separation in maintained.
But, what triggers it?

## Slide 16
Fe plate
Min
15h30
4h30
1h30
30min
5 mm

## Slide 17
Discussion

## Slide 18
Pure Fe, 0.05M NaCl
Other
metals and alloys
Other enviroments
pH, NaCl conc.

## Slide 19
What if more defects?
Critical factors
Evans
Agar
Hoar
Akimov
Tomashov
Wagner number analysis
L =  Rp
1x1 mm2
1x1 cm2
1x1 dm2
1x1 m2
Pure metal or alloy?
Phases, intermetallics, precipitates, impurities, surface preparation, temperature gradients, crystal vibrations.
Solution: compositional variations (O2, Cl-, other conc.), conductivity, temperature gradients, convective fluxes, vibrations.
Heterogeneities
Solution composition
Conductivity
pH
Passivity
Time
Geometry (size and distances)

## Slide 20
M. Pourbaix, Lições de Corrosão Electroquímica, Lisboa, 1986.
Same metal/alloy
Different environment (pH)
10-2 M Cl-

## Slide 21
H. Kaesche, Corrosion of metals, Springer-Verlag, 2005.
Different metals
NEUTRAL
CONDITIONS
Cu
Fe
Fe
Mg

## Slide 22
Effect of distance
N.D. Tomashov, Theory of Corrosion and Protection of Metals, Macmillan, 1966.

## Slide 23
Other metals
AZ31
minutes
30 min
20 hours
1 mm
Pure Zinc
1 hour
12 hours
500 μm
Coatings and deffects

## Slide 24
Other metals
Zinc
18 hours
1 hour
mins
Mg
13 hours
mins
30 min
2h
Twin wires
polished
AA2024
1 hour
17 hours
1 mm

## Slide 25
Plates
Other metals
Zinc
1 h
6 h
24 h
5 mm
AA2024
etched
4 h
12 h
5 mm
AA2024
polished
4 h
12 h
5 mm
Mg
min
30 min
1 h
5 mm

## Slide 26
Conclusions
The anode/cathode separation is explained by the different local pH which maintains one electrode active while the other becomes passive.
Still not clear is what provokes the pH separation at the beginning of immersion.
There is a critical distance beyond which this effect ceases. Which distance and the parameters that control it remain unidentified.

## Slide 27
Acknowledgements
M.C. Quevedo thanks CONACYT (Mexico) for the post doc scholarship approach nº 203529 and A.C.Bastos thanks a post-doc grant with the reference BPD/UI50/2739/2013. Funds from Fundação para a Ciência e a Tecnologia (Portugal) project PTDC/CTM-MAT/1515/2012 are also acknowledged.

## Slide 28
Dimensional causes of discrepances
Same current density
Change conductivity
accordingly
Conc. O2

## Slide 29
Wagner number
(L)
Wagner Length
Wagner Parameter
Polarization Parameter
Wagner Number (W)
In scalling, the Wagner number must be kept constant
Waber
Small value
Current varies significantly over
The surface of the electrode
Large value (W)

Microscopic
behaviour
Macroscopic
behaviour



Small variation in current density at electrode surface


Localized corrosion
Uniform corrosion